Neutron scattering study of tantalum monohydride and monodeuteride

Mikhail A. Kuzovnikov, Vladimir E. Antonov, Alexandre S. Ivanov, Thomas Hansen, Stanislav Savvin, Valery I. Kulakov, Marek Tkacz, and Alexander I. Kolesnikov

Table S1. Crystal structures and coordination environment of various tantalum hydrides and deuterides.

| Phase | Source | Space group, lattice parameters and atomic coordinates | Shortest interatomic distances, Å |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Ta-Ta | Ta-H | H-H |
| TaHx (solution) |  | Im-3m, a=3.301Å Ta 0 0 0 H 1/4 1/2 0 | 2.86 | 1.85 | n/a |
| Ta2H(D) | [11,12] | C222, a=4.77Å b=3.37Å c=4.77Å Ta 1/4 1/4 0.262 H 0 0 0 | 2.83 | 1.92 | 2.92 |
| Ta3H(D)2 | [12] | C2221, a=14.41Å b=3.40Å c=19.21Å Ta1 11/12 3/4 9/16 Ta2 11/12 1/4 11/16 Ta3 3/4 3/4 3/16 Ta4 3/4 1/4 1/16 Ta5 11/12 3/4 1/16 Ta6 11/12 1/4 3/16 H1 1/2 0 1/8 H2 2/3 1/2 1/8 H3 5/6 0 1/8 H4 1/2 0 3/4 H5 5/6 0 0 | 2.94 | 1.90 | 2.40 |
| Ta4H(D)3 | [13,14] | I222, a=4.82Å b=9.64Å c=3.41Å Ta 0.25 0.121 0.75 H1 0 0.26 0 H2 0 0 0 | 2.95 | 1.89 | 2.59 |
| TaD0.87 | [24,34] | Cccm, a=4.79Å b=3.46Å c=4.83Å Ta 1/4 1/4 0 H 0 0 1/4 | 2.95 | 1.91 | 2.42 |
| TaH0.89 | present | see Table 4 | 2.96 | 1.91 | 2.41 |
| TaD0.96 | present | see Table 2 | 2.96 | 1.91 | 2.40 |
| TaH2.2 | [7] | P63mc, a=3.223Å c=5.143Å Ta 1/3 2/3 1/4 H1 0 0 0.876 H2 1/3 2/3 0.631 | 3.17 | 1.96 | 2.25 |
| TaH3 | [26] | I-43d, a=7.707Å (0 GPa, calculated with DFT) Ta 0.954 0.954 0.954 H 0.954 0.455 0.611 | 3.22 | 1.92 | 1.96 |