SUPPLEMENTARY MATERIAL

to the manuscript

Reversible hydrogen storage in multilayer graphane: lattice dynamics, compressibility, and heat capacity studies

by

Volodymyr A. Yartys a, Vladimir E. Antonov b, Boris M. Bulychev c, Vadim S. Efimchenko b, Valery I. Kulakov b, Mikhail A. Kuzovnikov d, Ross T. Howie d, Hannah A. Shuttleworth d, Mylaine Holin d, Rebecca Rae d, Matthew B. Stone e,

Boris P. Tarasov f, Radion I. Usmanov g,b, Alexander I. Kolesnikov e,*

a Institute for Energy Technology, P.O. Box 40, Kjeller NO-2027, Norway

b Institute of Solid State Physics RAS, 142432 Chernogolovka, Moscow District, Russia

c Moscow State University, Leninskiye Gory, 119991Moscow, Russia

d Centre for Science at Extreme Conditions and School of Physics and Astronomy,

University of Edinburgh, Edinburgh EH9 3FD, United Kingdom

e Neutron Scattering Division, Oak Ridge National Laboratory, Oak Ridge, TN 37831, USA

f Institute of Problems of Chemical Physics RAS, 142432 Chernogolovka, Moscow District, Russia

g National Research University Higher School of Economics, 20 Myasnitskaya ul., 101000 Moscow, Russia

Fig. S1. Contour plots of the dynamical structure factor S(Q,E) of graphite hydride measured with the SEQUOIA neutron spectrometer at T = 5 K using four incident neutron energies Ei = 55, 120, 220, and 420 meV.

Fig. S2. Contour plots of the dynamical structure factor S(Q,E) of graphite deuteride measured with the SEQUOIA neutron spectrometer at T = 5 K using four incident neutron energies Ei = 55, 120, 220, and 420 meV.

Fig. S3. The experimental X-ray pattern of a CD1.06 sample (solid squares) and results of its semi-quantitative profile analysis in the framework of the P63mc and  space groups (solid curves) [6]. The c-parameter of the  structure is twice as small as that of the P63mc structure. The intensity distribution among the diffraction lines in the angular range 30 < 2θ < 50° can semi-quantitatively be reproduced in the P63mc space group (graphane II structure), whereas the  group (graphane I structure) gives a qualitatively inadequate distribution.

Fig. S4. The ratio EH/ED of the energies of peaks in the acoustic part of the phonon densities of states gcalc(E) calculated for the graphane II phases of graphite hydride and deuteride (see Fig. 6b). The dashed line shows a linear fit to the data points.

Fig. S5. Electronic band structure and density of states (right panel) of the graphane II phase of graphite hydride according to LDA calculations. Results of this paper.

Fig. S6. (a) and (b): Experimental values a(T) and c(T) of the lattice parameters of graphite hydride at ambient pressure (blue circles) approximated by dependences analogues to Equation (3) (blue curves) with the fitting parameters indicated in the insets.

(c): Experimental values of the c/a ratio (blue circles) and a blue curve calculated as cfit(T)/afit(T) using the cfit(T) and afit(T) dependences from figures (a) and (b), respectively.

Fig. S7. The difference  between the heat capacities at constant pressure and constant volume calculated for graphite hydride using Vfit(T) from Fig. 14 and fit(T) and βfit(T) from Fig. 15.

[6]	V.E. Antonov, I.O. Bashkin, A.V. Bazhenov, B.M. Bulychev, V.K. Fedotov, T.N. Fursova, A.I. Kolesnikov, V.I. Kulakov, R.V. Lukashev, D.V. Matveev, M.K. Sakharov, Y.M. Shulga, Multilayer graphane synthesized under high hydrogen pressure, Carbon 100 (2016) 465–473, https://doi.org/10.1016/j.carbon.2015.12.051.