**HUMAN CELLS survivability as a function of**

**implant surface topography**

**Straumal B.B.1-4, Gornakova A.S.1**, **Kiselevskiy M.V.5, Anisimova N.Yu.5,**

**Nekrasov A.N.6,** **Kilmametov A.R.1,2, Strug R.E.7, Rabkin E. 7**

*1Institute of Solid State Physics, Russian Academy of Sciences, Chernogolovka, Russia*

*2Scientific Center in Chernogolovka, Russian Academy of Sciences, Chernogolovka, Russia*

*3Institute for Nanotechnology, Karlsruhe Institute of Technology (KIT), Germany*

*4National University of Science and Technology «MISIS», Moscow, Russia*

*5Laboratory of Cell Immunity “N. N. Blokhin National Medical Research Centre of Oncology” of the Health Ministry of Russia, Moscow, Russia*

*6Institute of Experimental Mineralogy, Russian Academy of Sciences, Chernogolovka, Russia*

*7Department of Materials Science and Engineering, TECHNION-Israel Institute of Technology, Haifa, Israel*

straumal@issp.ac.ru, erabkin@technion.ac.il

Titanium-based alloys are widely employed in biomedical applications (including bone replacing implants) due to their favourable combination of good mechanical properties and biocompatibility [1]. The latter depends not only upon chemical and physical properties of the implanted materials, but also on the interaction between the body cells and the material surfaces [1]. A variety of implant surface modification techniques was investigated in terms of their effect on implants biocompatibility [2], including classic metallographic grinding and polishing causing fine-grooved surface topography.

In this study we investigated the effect of surface topography on biocompatibility of the Ti-6%Al-4%V alloy (being known as VT6 according to GOST 19807-91). The surfaces with controlled and systematically changing roughness were obtained by mechanical grinding using a series of abrasive sandpapers, and by fine polishing with diamond pastes.

Surface topography of the samples was characterized by light microscopy and confocal microscopy, with the emphasis on quantitative evaluation of the roughness parameters according to ISO 25178. Biocompatibility was studied by HEK-293 cells adhesion onto the studied surfaces.

We demonstrated that abrasive paper grinding caused one-directional grooved surfaces, whereas the diamond paste polished surfaces appeared to be a superposition of significantly smooth areas with a regular network of deep pits.

Our biocompatibility (cell adhesion) results demonstrated that the fine abrasive paper (10-15 µm grain size) grinding, causing one-directional ordered grooved surface, is distinctly favourable for cell survivability, while the adhesion to smoothly polished surfaces appearss to be low.

*This work was carried out with the financial assistance of the Russian Foundation for Basic Research (grants 18-33-00473 and 19-58-06002) and Israel Ministry of Science and Technology (grant 3-16534).*

1. Kantesh Balani, Vivek Verma, Arvind Agarwal, Roger Narayan*. Biosurfaces: A Materials Science and Engineering Perspective*. John Wiley and Sons, 2015

2. K. Anselme & M, Bigerelle. Role of materials surface topography on mammalian cell response, *International Materials Reviews*, 2011, vol. 56, issue 4, pp. 243-266